| Table G.10 - Severity Descriptions |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item | Severity |  |  |  |  |  |
|  |  | 1 |  | 2 | 3 | 4 | 5 |
| 1 | Metalwork | .1 | No signs of rusting or damage | Minor surface rusting | Moderate pitting | Deep pits and perforations ( localised sever corrosion) | Disintegrating by corrosion mechanisms |
|  |  | .2 | No loss of section thickness | Minor section loss (penetration less than 5% of section) | Moderate section loss causing some reduction in functionality (penetration 5 to 20% of section thickness) | Major section loss causing significant reduction in functionality (penetration more than 20% of section) | Collapsed or collapsing |
|  |  | .3 | No signs of rusting or damage to bolts, nuts and rivets | Non structural bolts loose, minor corrosion of nuts and washers | Non structural bolts missing, moderate corrosion of rivet heads, nuts and washers | Structural bolts missing, rivets loose or missing, crack through bolt | Failure of element due to missed/failed bolts/rivets |
|  |  | .4 | No corrosion or damage of weld runs | Slight corrosion of weld run | Crack at toe of weld, moderate reduction in size of weld due to corrosion | Longitudinally cracked weld, major reduction in size of weld due to corrosion | Weld connection failure (longitudinal crack) |
| 2 | Reinforced Concrete, Prestressed Concrete & Filler Joist | .1 | No spalls | Minor localised spalls exposing shear links | Major localised spalls exposing shear links and main bars with general corrosion | Joined up, deep spalls exposing shear links and main bars with general and pitting corrosion | Collapsed |
|  |  | .2 | Hairline cracks, difficult to detect visually | Cracks and crazing in areas of low flexural behaviour (cracks less than 0.3mm) | Cracks and crazing in areas of high flexure. Cracks approx' 1mm and easily visible | Wide/deep cracks (more than 2mm). Shear cracks | Element unable to function due to structural cracks |
|  |  | .3 | No signs of damage to prestressing | Substandard grouting of ducts (may not be visible) | Cracks along line of prestressing duct | Exposed prestressing cables | Failed prestressing cables |
|  |  | .4 | No signs of delamination | Early signs of delamination e.g. cracks with rust staining | Delamination in areas of low flexural and/or shear action | Delamination in areas of high flexure and/or shear action | Failure due to delaminated bars |
|  |  | .5 | No signs of thaumasite or freeze-thaw attack | Slight cracking caused by thaumasite or freeze- thaw | Moderate thaumasite or freeze-thaw attack | Major thaumasite or freeze-thaw attack | Failure due to thaumasite or freeze- thaw attack |

| Table G.10 - Severity Descriptions (continued) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item | Severity |  |  |  |  |  |
|  |  | 1 |  | 2 | 3 | 4 | 5 |
| 3 | Masonry, Brickwork & Mass Concrete | .1 | No evidence of deformation | Minor deformation | Moderate deformation | Major deformation | Collapsed |
|  |  | .2 | Pointing sound | Minor depth of pointing deteriorated | Moderate to significant depth of pointing lost, but does not appear to be rapidly disintegrating or crumbling, bricks not easily loosened | Pointing in very poor condition, severely weathered, crumbling to touch and/or significant depth loss, bricks easily loosened | Collapsed |
|  |  | .3 | No arch ring cracking or separation | Arch ring cracks difficult to see | Arch ring separation (gap less than 25mm) | Arch ring separation (gap greater than 25mm) | Disintegrated |
|  |  | .4 | No arch barrel cracks | No diagonal cracks, longitudinal cracks less than 3mm wide, lateral cracks | Diagonal cracks, longitudinal cracks greater than 3mm wide | Diagonal cracks, longitudinal cracks breaking barrel into 1m sections or less | Arch barrel failure |
|  |  | .5 | No cracks | Minor hairline cracks and shallow spalls | Moderate cracks (easily visible, crazing) and deep localised spalls | Major cracks and spalling | Failure due to structural cracks |
|  |  | .6 | No bricks/masonry blocks missing, minor surface weathering | Few bricks/stones missing (no adjacent ones missing), major surface weathering | Moderate loss of bricks/stones | Severe loss of bricks/stones | Failure due to missing stones/bricks |
|  |  | .7 | No bulging, leaning or displacement | Minor bulging, leaning or displacement | Moderate bulging, leaning or displacement | Severe bulging, leaning or displacement | Collapsed or non functional |
| 4 | Paintwork and Protective Coatings | .1 | Finish coat sound, slight weathering | Normal weathering of finishing coat | Spot, chips and cracks of the finishing coat, undercoat exposed but sound | Failure of finishing coat and spots, chips and cracks to undercoat/substrate | All coats failed |

| Table G.10 - Severity Descriptions (continued) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item | Severity |  |  |  |  |  |
|  |  | 1 |  | 2 | 3 | 4 | 5 |
| 5 | Vegetation | .1 | Slight to no vegetation | Minor vegetation causing no structural damage (surface mosses, small grass and weeds) | Vegetation growth on or near bridge causing structural damage and/or deformation e.g. roots and branches of nearby trees, small tree/plants growing on structure | Vegetation growth on or near bridge causing major structural damage and/or deformation e.g. roots and branches of nearby trees, large tree growing on structure | Failure caused by vegetation growth or a tree collapsing on the structure |
|  |  | .2 | Slight to no vegetation | Low depth/density of vegetation cover, easily removed | Significant depth/density of vegetation, obscuring inspection e.g. ivy | Inspection impossible due to vegetation growth but structural damage due to vegetation unlikely | Inspection of critical structural elements not possible due to density of vegetation and rot systems likely to be causing structural damage |
| 6 | Foundations | .1 | No visible settlement of structure | No visible settlement, but cracks may be due to it | Minor settlement of structure | Major settlement of structure | Collapsed due to settlement |
|  |  | .2 | No visible differential movement of structure | No visible movement, but cracks may be due to it | Minor differential movement of structure | Major differential movement of structure | Collapsed due to differential movement |
|  |  | .3 | No visible sliding of structure | No visible sliding, but cracks may be due to it | Minor sliding of structure | Major sliding of structure | Collapsed due to sliding |
|  |  | .4 | No visible rotation of structure | No visible rotation, but cracks may be due to it | Minor rotation of structure | Major rotation of structure | Collapsed due to rotation |
|  |  | .5 | No scour | Minor scour | Moderate scour | Major scour | Dangerous scour or failure |
|  |  | .6 | Substructure appears unaffected by foundation faults (assume no foundation faults) | Foundation faults causing minor cracks in substructure | Foundation faults causing moderate cracking in substructure | Foundation faults causing major cracks and deformation in substructure | Failure due to foundation faults |

| Table G.10 - Severity Descriptions (continued) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item | Severity |  |  |  |  |  |
|  |  | 1 |  | 2 | 3 | 4 | 5 |
| 7 | Invert, apron & river bed (also see 2 and 3) | .1 | No scour | Minor scour | Moderate scour | Major scour | Dangerous scour or failure |
|  |  | .2 | No vegetation growth or silting | Vegetation growth, trapped debris and silting causing slight disruption to flow | Vegetation growth, trapped debris and silting, significant disruption to flow causing faster flow in areas of river | Vegetation growth, trapped debris and silting severe disruption to flow causing much flow in areas of the river | Failure caused by vegetation growth, trapped debris and silting |
| 8 | Drainage | .1 | In sound condition and fully functional | Mostly functional (less than 25% of cross section blocked) | Part functional (25% to 50% of cross section blocked) | Mostly non functional (more than 50% of cross section blocked) | Totally blocked/non- functional/broken |
|  |  | .2 | Causing no staining | Causing minor staining | Cleaning of staining required | Urgent cleaning required | Urgent & frequent cleaning |
|  |  | .3 | No structural damage | Causing minor structural damage | Causing structural damage | Causing major structural damage | Causing severe damage to adjacent elements |
|  |  | .4 | No blockage of weep holes, outlets | Minor blockage of weep holes, outlets | Moderate blockage of weep holes, outlets | Major blockage of weep holes, outlets | Non functioning weep holes |
| 9 | Surfacing | .1 | Little to no wear and weathering | Minor wear/weathering | Moderate wear/weathering | Major wear/weathering | Dangerous |
|  |  | .2 | No crazing, tracking or fretting | Minor crazing, tracking and/or fretting | Moderate crazing, tracking and/or fretting | Major cracks, tracking and/or fretting | Complete break up |
|  |  | .3 | Dense | Poor texture | Open texture | Very open texture | Dangerous |
|  |  | .4 | Sound | Cracks in top layer | Top layer breached | Deep cracks and potholes | Top layer completely missing |
|  |  | .5 | Not slippery | Starting to become slippery | Definitely becoming slippery | Slippery | Dangerous |
|  | Flagged Surfacing | .6 | No defects | Trips <5mm | Cracked flags Trips > 5mm and < 10mm | Trips > 10mm and <20mm | Trips > 20mm |

| Table G.10 - Severity Descriptions (continued) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item |  | Severity |  |  |  |  |  |
|  |  |  | 1 |  | 2 | 3 | 4 | 5 |
| 10 | Expansion Joints | Asphaltic Plug | .1 | Sound | Minor debonding between plug and road | Moderate debonding between plug and road | Major debonding between plug and road | Dangerous |
|  |  |  | .2 | Sound | Slight loss of surface binder and aggregate | Loss of aggregate (surface penetration 20 to 50mm) | Loss of material from joint (causing holes > 50mm deep) | Missing |
|  |  |  | .3 | Sound | Minor tracking and flow of binder | Moderate tracking and flow of blinding | Major tracking and flow of binder | Disintegration |
|  |  | Nosing Defects | .4 | Sound | Minor cracking along nosing | Moderate cracking along nosing, some break-up | Break up of nosing material | Disintegration |
|  |  | Elastomeric and others | .5 | Minor signs of wear | One bolt missing at cross section | Numerous bolts missing at cross section | Majority of bolts missing at a cross section | Failure due to missing bolts |
|  |  |  | .6 | Strip sealant sound | Strip sealant loose/poor, compression seal dropped and/or worn | Sealant breached, strip sealant breached | Sealant missing, strip sealant missing/out | Failure |
|  |  |  | .7 | Sound road surface adjacent to joint | Minor break up of road surface adjacent to joint | Moderate break up of road surface adjacent to joint, some debris in joint seal | Major break up of road surface adjacent to joint, significant debris in joint | Joint failure due to deteriorated condition of adjacent road surface |
|  |  |  | .8 | Sound fixings | Bolt sealer missing | Fixings loose | Fixings missing, plates and angles loose | Failure due to missing fixtures |
|  |  |  | .9 | Sound components | Initiation of cracking or tearing of components | Crack/tear <20% of width of component | Crack/tear >20% but <50% of width of component | Failure of expansion joint components |
|  |  | Buried Joint | .10 | Reasonably sound | Minor surfacing cracking | Moderate surfacing cracking | Major surface cracking | Failure |
|  |  |  | .11 | Sealant for induced crack is sound | Minor cracking or break up of sealant for induced crack | Moderate cracking or break up of sealant for induced crack | Major cracking or break up of sealant for induced crack | Disintegrated or missing sealant for induced crack |
|  |  | Joint leakage | .12 | No visible signs of leakage | Minor leakage through joint | Moderate leakage through joint | Major leakage through joint causing structural damage | Open joint causing major structural damage |

| Table G.10 - Severity Descriptions (continued) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item | Severity |  |  |  |  |  |
|  |  | 1 |  | 2 | 3 | 4 | 5 |
| 11 | Embankments | .1 | Sound. No deformation | Minor subsidence. Minor deformation | Minor slip/settlement causing slight cracking of carriageway | Major slip/settlement causing major cracking of carriageway | Critical slip/settlement |
| 12 | Bearings (also see 1) | .1 | Negligible rusting, minor weathering | Minor rusting, moderate weathering | Moderate rusting | Major rusting | Failed or seized due to rusting |
|  |  | .2 | Correct position | Minor offset | Moderate offset/tilt | Dislodged | Off bearing/missing |
|  |  | .3 | Sliding bearing in correct position | Sliding bearing in slightly skewed (off centre) position at normal temp | Sliding bearing at end of travel in normal temperatures | Sliding bearing beyond designed extent of travel at normal temperatures | Sliding bearing failed |
|  |  | .4 | No crazing | External crazing | External breakdown | Major breakdown (PTFE, laminations, rubber etc.) | Complete breakdown |
|  |  | .5 | Sliding plate sound | Minor deformation of sliding plate | Moderate deformation of sliding plate | Major deformation of sliding plate | Bearings seized by sliding plate deformations |
|  |  | .6 | Bearings sound | Minor cracks | Moderate cracks or loose | Splitting and deformation | Disintegrated |
| 13 | Impact damage | .1 | No damage | Slight surface scoring, minor displacement of element e.g. marking and chipping of beam faces, several bricks across arch barrel width, slight impact deformation of steelwork | Moderate displacement of element e.g. beam slightly offset on bearings, significant number of bricks knocked out across arch barrel width, moderate impact deformation of steelwork | Severe displacement of element e.g. beam dislodged off bearings, many bricks knocked out across arch barrel width, major impact deformation of steelwork | Knocked down, broken, collapsing |
| 14 | Waterproofing (try to exclude leaks through joints) | .1 | No visible sign of seepage | Minor seepage through deck/arch etc. (slow dripping) | Moderate seepage through deck/arch etc. (some resistance to seepage) | Major seepage (little resistance) through deck/arch etc. causing structural damage | Non-functional Causing critical structural damage |
|  |  | .2 | No visible sign of seepage | Damp surface, slight water stains on soffit | Wet surface, drops of water falling and significant staining | Very wet surface and stalactites causing structural damage | Major structural damage caused by waterproofing not functioning properly |

| Table G.10 - Severity Descriptions (continued) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item | Severity |  |  |  |  |  |
|  |  | 1 |  | 2 | 3 | 4 | 5 |
| 15 | Stone Slab Bridges | .1 | Sound, no defects or damage | Minor cracking | Moderate cracking but no visible displacement | Major cracking and/or displacement | Collapsed |
| 16 | Timber | .1 | No sign of damage | Minor signs of damage | Moderate signs of damage | Major signs of damage | Disintegrated through damage |
|  |  | .2 | No loss of section | Minor section loss (decay less than 5% of section) | Moderate section loss causing some reduction in functionality (decay 5 to 20% of section thickness) | Major section loss causing significant reduction in functionality (decay more than 20% of section thickness) | Collapsed or collapsing |
|  |  | .3 | No visible signs of open joints | Joints/shakes open slightly on surface or cracked coating at joints/shakes | Open joints/shakes < 50% width beam, in areas of low flexure or < 25% in areas of high flexure | Open joints/shakes < 50% width beam, in areas of low flexure or < 25% in areas of high flexure | Beam separated into multiple elements |
|  |  | .4 | No signs of rusting or damage to fixings | Non structural bolts loose, minor corrosion of fixings | Non structural bolts missing, moderate corrosion of fixings | Structural fixings missing | Failure of element due to missed/failed fixings |

The column headed "Def" on the inspection pro forma is for the Defect Type e.g. "3.2" for masonry pointing. If there are no defects then insert "0"

Note: Item No. 10 for Expansion Joints within Table G10 Severity Descriptions has been replaced with Items 17 and 18 as below. The replacement is fully described in the TfL documents ‘Inspection guidance for bridge expansion joints’ Volumes 1 and 2.

Additional items have been added to describe other defects common to Transport for London structures.

| Table G.10 - Severity Descriptions (continued) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No | Item | Severity |  |  |  |  |  |
|  |  | 1 |  | 2 | 3 | 4 | 5 |
| 17 | All Joint Types |  |  |  |  |  |  |
|  | Joint leakage | .1 | The area below the expansion joint shows no sign of water or water staining. This includes the underside of the deck, the bearing shelf and the abutment wall. | Small amounts of water appear to be leaking from the expansion joint. There is no apparent damage to other parts of the structure. | Noticeable volumes of water are passing through the expansion joint, and there is now a reasonable expectation that durability of the structure will be affected. Damage is occurring to protective systems such as the paint system. | High volumes of water are draining through the expansion joint, causing some minor structural damage, including minor corrosion to the bearings or bearing shelf. | The expansion joint is open and water is freely passing from the carriageway through the expansion gap. Corrosion is significant to the bearings, bearing shelf or abutment. |
|  | Joint sub-surface drainage | .2 | Joint drainage appears to be functioning correctly. There are no signs of ponding adjacent to the expansion joint. Outlets for the drainage are clear. | The outlets to the drainage are slightly blocked, but there is no obvious sign of ponding on the carriageway by the expansion joint. | There are signs of ponding on the carriageway by the expansion joint, but they are not extensive. The outlets are partially blocked. | Surface water on the carriageway is significant. The drainage outlets are almost fully blocked (>75%). | Joint drainage is completely non-functional. Ponding is severe. The drainage outlets appear blocked. |
|  | Adjacent road surfacing | .3 | The road surfacing adjacent to the joint is in as-new condition, with no cracks, tracking or rutting. | There is some cracking, but this is not affecting the ride quality, or exposing any part of the joint. | The road surfacing is significantly cracked, but there are no pot-holes, nor is any part of the joint exposed. | The cracking is such that pot-holes are expected to form shortly. The joint or nosing is becoming exposed. | The surfacing has disintegrated, exposing the nosing or the joint component. There may be leakage. |
|  | Fixtures | .4 | All plates and cover plates are in good condition, securely attached. | A plate is slightly defective, either bent or loose, but it is not causing any loss of functionality or a hazard. | A plate is significantly loose or heavily damaged, but is generally functional and is not causing a hazard. | A plate is missing, but not causing a significant hazard, but may affect durability in the long term. | A plate is missing or sufficiently loose to cause a significant hazard. |
|  | Joint vegetation | .5 | There is no vegetation growing from any part of the expansion joint, either in the carriageway, verge, reserve or from underneath. | Small, insignificant amount of vegetation are growing from the joint, and are causing no hazard or not affecting functionality. | Small amounts of vegetation are growing from the joint, and are causing a limited inconvenience, for example to pedestrians. | Vegetation is present in the joint and is fairly widespread, causing inconvenience and reduced durability of the joint. | There is a significant amount of vegetation growing from the expansion joint, causing corrosion to the joint. |

| Buried joint |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 6 | Surfacing over buried joint | The presence of the joint is not obvious from the surface (except for the sealed saw-cut, if present). There are no defects to the carriageway surfacing or verges/ footways /reserve over the joint. | There are some cracks in the surfacing over the joint, but these cracks are very narrow and shallow (max depth 25mm). | The cracks are clearly visible, up to but not exceeding 5mm in width at the extreme. The depth of the crack is less than 50mm. There is no evidence of water leakage. | Cracks have developed, up to 25mm in width at the extreme. The depth of the crack is less than the depth of the surfacing. | The width of the crack is greater than 25mm and the depth is similar to the depth of the surfacing. The surfacing around the cracks is breaking up. There is evidence of leakage. |
| 7 | Crack inducer sealant | The sealant in the saw-cut is fully present, fully bonded to each side of the crack and is not raised above the surfacing level. | The seal has some cracks, which are hairline and short, and do not affect the integrity of the seal. The seal has not been pushed upwards to any noticeable degree. | The cracks are clearly visible, or some of the seal is unbonded. Generally, it is still functional. | There is major cracking of break up of the sealant, so it can no longer be considered fully functional. | The seal is completely missing at some point, causing break up of the adjacent but unsupported surfacing. |
| Asphaltic plug joint |  |  |  |  |  |  |
| 8 | Plug debonding | The plug/ surfacing interface is bonded, with no gap evident, at any point across the carriageway, verge, reserve or footway. | The plug has debonded from the surfacing at some point across the carriageway, but the gap is still narrow (1- 2mm). The depth of the debonded area is maximum 25mm. The adjacent road surface remains in good condition. | The debonded gap is now significant. The adjacent road surfacing is unsupported in the affected areas and has potential to start breaking up under traffic loading. The gap is around 5mm wide and the depth is less than 50mm. | The debonded gap is now greater, there are visible signs of the adjacent surface breaking up because it is now clearly unsupported. The gap is greater than 5mm wide but the depth is less than the depth of the surfacing. There is some leakage evident. | The joint is now sufficiently debonded that the adjacent surfacing is breaking up due to lack of support. The plug material is also damaged as the leading edge is unprotected. The debonded area is to the full depth of the surfacing. The joint is leaking as a result. |
| 9 | Loss of plug material | The plug is 100% intact, with no missing material. | A small amount of material is missing, with shallow holes in the plug (<20mm penetration). There is very little effect on ride quality or very little noise produced. | There is significant loss of material, with penetration up to 50mm. Ride quality is affected and noise is produced. | There is a serious loss of material, with holes deeper than 50mm. There is some leakage evident. | Some of the joint is missing to the full depth of the plug, or the plug is broken up as a result of missing material. The joint is leaking. |
| 10 | Tracking and flow of material | The plug follows the alignment of the adjacent surfacing, which is untracked, with no flow of plug material onto it. | Slight depressions in the plug are visible on inspection, but are not significant, or some plug material has flowed beyond the boundary. The effect is purely aesthetic. | Tracking is clearly visible or a significant amount of binder has flowed onto the adjacent surfacing. Where tracking has occurred, there are small mounds of displaced material at the edges of the carriageway. | A very large amount of binder has flowed, or tracking is serious, generating significant mounds at the edges of the carriageway. | The tracking or flow of material has occurred to such an extent that the joint has disintegrated. The joint is leaking. |

| All other joint types |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| 11 | Nosing defects | Reinforced elastomeric |  |  |  |  |
|  |  | The transition strip is in an as-new condition, and is completely bonded to the joint and adjacent surfacing and is completely uncracked. | Cracks in the transition strip are visible on close inspection, but are having no effect on joint functionality. | The cracking is extensive, leading to some break up of the material or the transition strip is no longer fully bonded to the surfacing or joint. | Cracking has developed sufficiently that the transition strip has broken up, with some material missing from the strip. The joint component is becoming exposed. | The nosing material is beyond isolated break up – it has disintegrated, leaving other elements of the joint exposed. The joint is leaking. |
|  |  | Elastomeric in metal runners (resin-encapsulated) |  |  |  |  |
|  |  | The resin strip is in as new-condition (see above). | Cracks are visible on close inspection, but there is no effect on joint functionality. | Cracking of the strip is fairly extensive. Some functionality remains – the surfacing is generally supported and the rails are generally protected. | Isolated areas of the resin have broken up, leaving parts of the rails unprotected and some of the adjacent surfacing unsupported. | The resin has disintegrated sufficiently to expose the reinforcement embedded in the resin, as well as leaving the rails and adjacent surfacing unprotected. The joint is leaking. |
| 12 13 14 | Missing or loose bolts | No bolts are missing or loose. There is no more than minor wear to the bolts. | A maximum of one bolt is missing/loose at any cross section of the joint, and this one missing bolt is not causing failure. | More than one bolt is missing/loose and up to half are missing/loose at a particular cross section. This severity class will only apply where there are more than two bolts at any cross section of the joint. | At any particular cross section of the joint, more than half of the bolts are missing/loose, but this is not causing failure. | The joint has failed due to missing/loose bolts, regardless of how many are missing/loose. |
|  | Seal | The seal appears in good condition, with no breaches, cracks or tears. It is securely attached on both sides. No debris is present in the seal. | The seal has some cracks, or very minor tears or breaches, but is still able to function to a large extent. The defects require close inspection to see. There is a small amount of debris in the seal. | The seal is visibly breached, allowing some water through the joint. There is a small amount of debris in the seal. | The seal is missing or significantly breached at least at some point across the joint. It does, however, retain some functionality. There is evidence of water leakage. The seal is holding a significant amount of debris. | The seal is missing or sufficiently disintegrated to allow large amounts of water to flow through the joint. The seal is full of debris. |
|  | Components | Reinforced elastomeric |  |  |  |  |
|  |  | All joint components are in good condition, with no visible signs of defects. There are no cracks or tears visible. | Cracks or tears are visible. They are hairline, and require careful inspection to detect. | Cracks or tears are easily visible, but the joint is still able to function. | Cracks or tears are significant, but there remains some limited functionality. The steel in the plates is exposed. Complete failure is expected shortly. | A component has completely failed. Part of it has detached or is missing. A steel plate is loose or missing. |

|  |  |  | Elastomeric in metal runners |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | The rails are in good condition. They are straight, level and flush with adjacent surfacing. There are no cracks in the rails. | The rails are generally in good condition, but on close inspection there are very slight deformities in the rails, but no vertical deflection. | A rail is clearly deformed, but is still able to function safely. There is no vertical deflection of the rail. | There has been some limited vertical deflection of the rail, or there are short hairline cracks in the rail. | A rail has completely cracked, is missing, has dropped due to failure of the supporting mechanism below or there has been significant vertical upward deflection of the rail, which is now likely to be pulled up by passing vehicles. |
|  |  |  | Steel comb/tooth |  |  |  |  |
|  |  |  | The comb components are in good condition, with no corrosion or cracks. There is no deformation of teeth. | The teeth are showing minor signs of corrosion, but no cracks are visible. Any loss of section is unidentifiable and there is no deformation of any teeth. | The teeth are moderately corroded with very minor loss of section (<5%). There is no limitation of movement and there are no signs of cracks or deformation of the teeth. | The teeth are severely corroded with significant loss of section (<20%), or there is some deformation but not to the extent where movement is restrained or traffic is affected. | At least one tooth has fractured, or the teeth are sufficiently misaligned so that movement will cause interference, or there is a crack in the metalwork. Corrosion has caused a serious loss of section of a tooth (>20%). |
| 18 | 1 | Movement/ construction joints | Seal is well bonded, uncracked, non-protruding and fully present along the whole length of the joint. | Seal is unbonded, cracked, or has been pushed out, but the joint retains a significant amount of functionality. | Joint displacement which is not in the designed plane of movement. Joint has not lost its functionality. | Significant amount of joint displacement which is not in the designed plane of movement. Joint approaching failure. | Extreme ‘out of plane’ displacement. Joint failed/non functional. |
| 19 | 1 | Graffiti | No graffiti | Non offensive graffiti out of sight of the general public | Low levels of non offensive graffiti within public view | High levels of non offensive graffiti within public view | Offensive Graffiti |
| 20 | 1 | Aesthetic Issues (possibly affecting long term durability eg. algae, lican, moss, leachate, efflorescence, water staining, general staining, etc) | None, Low or Medium levels of aesthetic issues not visible to the public. Not significant to long term durability. | High levels of aesthetic issues not visible to public and/or low levels visible to the public. Not significant to long term durability. | High levels of aesthetic issues in areas with low to moderate foot-fall. Affecting long term durability. | High levels of aesthetic issues in areas of high public footfall. Affecting long term durability. | Extreme levels of aesthetic issues which should be removed immediately. |

| 21 | 1 | Pigeon proofing/ Guano | None, insignificant defect to the pigeon proofing, insignificant deposits of guano | Missing spikes, small breaks in the mesh/netting or gaps at connections. Guano build up not noticeable by public but could affect durability of element. | Missing spikes and evidence of guano, breaks in netting large enough to allow avian access. Guano build up noticeable by the public. | Missing spikes and evidence of large volumes of guano affecting aesthetics and operative H&S. Large gaps in netting. Guano aesthetically affecting area accessed by public. | Issue of pigeon proofing likely to cause complaint from the public or Health and Safety concern (Cat 1). Large scale failure of netting. Guano which is causing H&S issues. |
| --- | --- | --- | --- | --- | --- | --- | --- |